DNA-directed Synthesis of Generation 7 and 5 PAMAM Dendrimer Nanoclusters

Youngseon Choi1, Almut Mecke2, Bradford Orr2,4, Mark Banaszak Holl3,4, and James R. Baker Jr.1,4*

1Department of Biomedical Engineering, School of Engineering, University of Michigan, Ann Arbor, MI 48109

2Department of Physics, School of Literature, Art and Science, University of Michigan, Ann Arbor, MI 48109

3Chemistry Department, School of Literature, Art and Science, University of Michigan, Ann Arbor, MI 48109

4Center for Biological Nanotechnology, Department of Internal Medicine, University of Michigan Medical School Ann Arbor, MI 48109-0648. www.nano.med.umich.edu.

*Corresponding author: James R. Baker Jr., M.D. jbakerjr@umich.edu; Ruth Dow Doan Professor and Director of Center for Biologic Nanotechnology, The University of Michigan Medical School, 9220 MSRB III, 1150 W.Med.Ctr.Dr., Ann Arbor, MI 48109-0648

ABSTRACT  A novel nanostructure was constructed using two different generations of polyamidoamine (PAMAM) dendrimers and complementary 50 base pair oligonucleotides.  The oligonucleotides were covalently conjugated to partially acetylated generation 5 and 7 PAMAM dendrimers, and analyzed using UV-vis spectroscopy.  These conjugates were then mixed at appropriate temperatures to allow for DNA-directed self-assembly of supramolecular arrays.  Overall size and shape of the DNA-linked dendrimer clusters was examined using tapping mode atomic force microscopy (AFM) to resolve the interspatial distance between the linked G7 and G5 dendrimer units.  The intra-dendrimer distance was measured to be 21  2 nm, which is in agreement with the theoretical length of the 50-base long oligonucleotide pairs.  In contrast, an AFM image of a mixture of non-complexed G7/G5 dendrimers only showed a few dendrimers physically in contact with a inter-dendrimer distance of 8 ~ 10 nm.  In addition, a dynamic light scattering (DLS) analysis of the cluster showed a diameter of 37  4 nm, which was the expected diameter of a DNA-linked dendrimer cluster.  These results suggest that PAMAM dendrimers can be self-assembled via complementary oligonucleotides to form supramolecular nanoclusters.

KEYWORDS. Oligonucleotide, DNA, PAMAM dendrimer, Self-assembly, Atomic force microscopy.Table of Contents Graphic

Figure. A representative three dimensional AFM image of a DNA-linked G7-G5 dendrimers on mica (80 nm  80 nm). The intra-dendrimer distance was measured to be 21  2 nm, which is in good agreement with the theoretical length of the 50-base long oligonucleotide duplex used to connect the polymers. A dynamic light scattering (DLS) measurement of a population of these clusters showed a mean diameter of 37  4 nm.

# Text boxes

262 nm3                           372 nm3                                 280 nm3

Figure 5. A few representative clusters in AFM images with their volumes and intra-dendrimer distances in good agreement of theoretical calculations of dimeric or trimeric self-assembly of G7 and G5 PAMAM dendrimer via DNA. The numbers below the image indicate the total volume based on a numerical integration method. The black bar indicates 20nm.

G5

G5

G7