# Applying Indium Oxide Nanowires as Sensitive and Specific Redox Protein Sensors

### Mahsa Rouhanizadeh*, a, Tao Tangb, Chao Lib, Gopikrishnan Soundararajan, Chongwu Zhoub, and Tzung Hsiaia

a Department of Biomedical Engineering and Cardiovascular Medicine, 
b Department of Electrical Engineering and Electro-physics,
University of Southern California, Los Angeles, CA 90089-USA

Indium Oxide nanowires have been found to demonstrate high sensitivity and specificity for detecting O3, Cl2, NO2, CO, H2. Low-density lipoprotein (LDL) initiates the development of heart disease. LDL particles, which harbor redox properties, can be modified from the reduced state to the oxidized state as one of the fundamental processes to coronary artery disease. Cytochrome C is an important electron transported in intracellular respiration. We hereby demonstrate Indium Oxide nanowire sensors as a potential sensor for detecting oxidatively modified LDL particles and cytochrome C.

We have built field effect transistors (FET) based on individual indium oxide nanowires of 10 nm in diameter.  The conductance of such transistors critically depends on their interaction with the environment, as oxidative or reductive species can significantly modulate the carrier concentration inside the nanowires. We have fabricated a PDMS microfluidic channel (2mm  in length, 360m in width by 100m in depth) in which the individual FET Indium Oxide Nanowire was exposed to water, LDL particles in both the reduced and oxidized states at 0.1 mg/mlit and cytochrome-c at 0.1 mg/milt in the reduced state. Precise flow rate at 10lit/min was delivered to the channel. The redox proteins were injected through a T-connection upstream. We obtained I vs. Voltage and Id vs. time curves for individual species.

We observed that that oxidized LDL generated higher conductivity than the reduced LDL particles. This differential level of conductivity was reproducible after repeated trials. Cytochrome C in its reduced form also demonstrated a distinct level of conductivity (Figure). Our study demonstrates the possibility of using Indium Oxide Nanowires as the sensitivity and specific sensors for detecting coronary artery disease.

References:

1.	Alex Sevanian, L.A., Ouliana Ziozankova, Low Density Lipoprotein (LDL) modification: Basic Concept and Relationship to Atherosclerosis. Blood Purification, 1999. 17: p. 66-68.

2.	C. Li, D.Z., X. Liu, S. Han, T. Tang, J. Han and C. Zhou, In2O3 nanowires as chemical sensors. Appl. Phys.Lett, 2003. 82( 1613).

3.	David C. Duffy, J.C.M., Olivier J.A.Schueller, George M.Whitesides, Rapid prototyping of Micro Fluidic Systems in Poly (dimethylsiloxane). Analytical Chemistry, 1998. 70(23).

4.	Kong, J.F., Nathan R.; Zhou, Chongwu, Chapline, Michael G., Peng Shu; Cho,Kyeongjae; Dai, Hongjie, Nanotube Molecular Wires as Chemical Sensors. Science, 1999. 287(5453): p. 622-625.